       2815A
High Grade   Double Side Tissue Tape
PRODUCT DESCRIPTION
2815A Double Sided Adhesive Tapes use non-woven tissue as carrier, coated with solvent acrylic adhesive on both sides, and protected with white double-sided PE coated silicone release paper.

Tape Composition

	Facing Composition
	Description
	Value (English)
	Value (Metric)

	Double Side Release Paper
	PE coated, White Color
	57 lbs / 3000 ft2
	100 gsm

	Adhesive
	Solvent Acrylic 
	42 lbs / 3000 ft2
	70 gsm

	Carrier
	Tissue
	8.4 lbs / 3000 ft2
	14 gsm

	Adhesive
	Solvent Acrylic 
	42 lbs / 3000 ft2
	70 gsm


TYPICAL PHYSICAL PROPERTIES
	PROPERTIES
	METRIC
	ENGLISH
	TEST METHOD

	Total Thickness
	150 Micron
	6 Mil
	PSTC-133 / ASTM D 3652

	Adhesion to Steel
	22 N/25mm
	79.2 Oz./In.
	PSTC-101 / ASTM D 3330

	Tack Rolling Ball
	5 cm
	2 In.
	PSTC-106 / ASTM D 3121

	Adhesion to Liner
	0.5 N/25mm
	1.8 Oz./In.
	PSTC-101 / ASTM D 3330

	Holding Power
	1000 Min./(25 mm x 25 mm).1kg
	1000 Min. 
	PSTC-107 / ASTM D 3654

	Service Temperature
	-30 ( +120 (C 
	-22 ~ +248 (F
	------------

	Applying Temperature
	+10 ~ 40 (C 
	+50 ~ +105 (F
	------------


TYPICAL APPLICATIONS: Suitable for general bonding, bag sealing, photos sticking, envelop sealing, shopping bag making, fabric / leather laminating, paper and film flying splicing, fabric positioning during computer embroidering, carpet fixing, foam laminating and die-cutting etc.

PRODUCT FORM & SIZE AVAILABLE

Cut Roll:  48 / 50mm (2") / 60 / 63mm (2.5") / 72 / 75mm (3") / 96mm / 100mm (4").
Log Roll:   1020/1240mm x 45 / 50m                Jumbo Roll: 1020/1240mm x 1000m /1250m
STORAGE & SHELF LIFE: 12 months when stored at 21(C (70(F) / 50% relative humidity out of direct sunlight. 

SURFACE PREPARATION: It is essential, as with all pressure-sensitive tapes, that the surface to which the tape is applied must be clean, dry, free of grease, oil or other contaminants.
PRODUCT USE: It is essential that the user evaluate the product to determine whether it is fit for a particular purpose and user’s method of application. Good results will be obtained when applied to a clean, dry surface with a suitable pressure on product between +10 ~ +40°C (+50 ~ +105 (F).   

LIMITED WARRANTY & LIMITED REMEDY: Your exclusive remedy & our obligation shall be, at our option, to replace or repair the our product or refund the purchase price of the product.
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